Contents

1.	STEEL SHEET MATERIAL (ENG)	2

1.1.	ZINCALUME® Ultra ACTIVATE™	2

1.2.	COLORBOND® Ultra ACTIVATE™	2

1.3.	SUMO™ 150Eq - ANTI FADING with 4 phases technology	2

1.4.	COLORBOND® FOR PANEL with ACTIVATE™ technology	2

1.4.1.	COLORBOND® FOR PANEL – COOL ROOM with ACTIVATE™ technology	2

1.4.2.	COLORBOND® FOR PANEL – CLEAN ROOM with ACTIVATE™ technology	2

1.4.3.	COLORBOND® FOR PANEL – ARCHITECTURAL WALL with ACTIVATE™ technology	2

1.5.	SUMO™ FOR PANEL with 4 phases technology	3

LỰA CHỌN NHANH NỘI DUNG BẰNG CÁCH:

- Ctrl + Click vào nội dung cần xem, hoặc

- Vào tab View/ chọn Navigation Pane / Chọn Heading/ Chọn vào nội dung cần xem

# STEEL SHEET MATERIAL (ENG)

## ZINCALUME® Ultra ACTIVATE™

ZINCALUME® Ultra STEEL with ACTIVATE™ technology is a hot-dipped aluminium/ zinc / magnesium alloy-coated integrated Activate™ technology AM150 with microstructure of 4 phases protection for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 150g/m2

Steel grade: G550 or G300 MPa  min (depend on profile)

Thickness: TCT:  ... mm

## COLORBOND® Ultra ACTIVATE™

COLORBOND® Ultra STEEL with ACTIVATE™ technology is a pre-painted steel on Zincalume® Ultra substrate – hot-dipped aluminium/ zinc / magnesium alloy-coated integrated Activate™ technology AM150 with microstructure of 4 phases protection for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 150g/m2 and meet pre-paint steel standard AS2728.

Steel grade: G550 or G300 MPa  min (depend on profile)

Thickness: APT:  ...mm

## SUMO™ 150Eq - ANTI FADING with 4 phases technology

SUMO™ 150Eq - ANTI FADING is a pre-painted steel hot-dipped aluminium/ zinc / magnesium alloy-coated with microstructure of 4 phases technology AM95 for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 95g/m2 and meet pre-paint steel standard AS2728.

Steel grade: G550 or G300 MPa  min (depend on profile)

Thickness: APT:  ...mm

## COLORBOND® FOR PANEL with ACTIVATE™ technology

## COLORBOND® FOR PANEL – COOL ROOM with ACTIVATE™ technology

COLORBOND® FOR PANEL - COOL ROOM with ACTIVATE™ technology is pre-painted steel for sandwich panel application in Cool room environment – hot-dipped aluminium/ zinc / magnesium alloy coated intergrated Activate™ technology AM150 with microstructure of 4 phases protection for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 150g/m2 and meet pre-paint steel standard AS2728.

Steel grade: G300 MPa min.

Thickness: APT:  ...mm

## COLORBOND® FOR PANEL – CLEAN ROOM with ACTIVATE™ technology

COLORBOND® FOR PANEL - CLEAN ROOM with ACTIVATE™ technology is pre-painted steel for sandwich panel application in Clean room environment – hot-dipped aluminium/ zinc / magnesium alloy coated intergrated Activate™ technology AM100 with microstructure of 4 phases protection for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 100g/m2 and meet pre-paint steel standard AS2728, integrated S.T.A.R.Vi antibacterial technology into the topcoat to kill 99.9% surface bacteria of finish good.

Steel grade: G300 MPa min.

Thickness: APT:  ...mm

## COLORBOND® FOR PANEL – ARCHITECTURAL WALL with ACTIVATE™ technology

COLORBOND® FOR PANEL - ARCHITECTURAL WALL with ACTIVATE™ technology is pre-painted steel for sandwich panel application in walling & roofing – hot-dipped aluminium/ zinc / magnesium alloy coated intergrated Activate™ technology AM100 with microstructure of 4 phases protection for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 100g/m2 and meet pre-paint steel standard AS2728.

Steel grade: G300 MPa min.

Thickness: APT:  ...mm

## SUMO™ FOR PANEL with 4 phases technology

SUMO™ FOR PANEL  is pre-painted steel for sandwich panel application – hot-dipped aluminium/ zinc / magnesium alloy coated with microstructure of 4 phases technology AM80 for superior corrosion resistance meet Australian standard AS1397, the minimum coating mass on both sides shall be 80g/m2 and meet pre-paint steel standard AS2728.

Steel grade: G300 MPa min.

Thickness: APT:  ...mm